## Slide 1: Enhanced Large-Scale Modeling of Additive Manufacturing: Layer-wise Equivalent Heat Flux Attribution for Thermal Interaction Analysis across Multiple Fabrications
Fan Chen, Dominik Kozjek, Conor Porter, Jian Cao
Email: fanchen@northwestern.edu
Supervisor: Jian Cao
March 24, 2025
17th USNCCM

## Slide 2
Chen F, Yan W. Materials & Design, 2020, 196: 109185.
Temperature history determines:
Residual stress
Fluid dynamics
Microstructure evolution
Part distortion
Defects
Mechanical properties
Metal additive manufacturing (AM) process:
Laser powder bed fusion
Directed energy deposition
Background
High-fidelity coupled CFD-FEM modeling
CFD
Coupled CFD-FEM
Two-layer two-track: high computational cost

## Slide 3
Part height:115 mm
Part height:50 mm
Part height:75 mm
Part height:125 mm
Experimental measurement
3500
2920
2330
1750
1170
580
0
-580
-1170
-1750
-2330
-2920
-3500
X-X strain component
(μstrain)
X-X strain component
(μstrain)
Accurate inherent strain pattern + Neutralization
Equivalent strain/temperature attribution [3,4] + element activation
Cooling
Relaxation
Temperature
Strain tensor
Equivalent layer
Large-scale FEM approaches in AM (1/2)
[11 Yi M, Xu B X, Gutfleisch O. Computational Mechanics, 2019, 64(4): 917-935.
[2] Cheng B, Shrestha S, Chou K. Additive Manufacturing, 2016, 12: 240-251.
[3] Olleak A, Xi Z. Manufacturing Letters, 2020, 24: 140-144.
[4] Liang, X., Chen, Q., Cheng, L., Hayduke, D., & Albert C. To (2019). Computational Mechanics, 64, 1719-1733.
Track-by-track heating + agglomeration
M Yi et. al. [1]
B Cheng et. al. [2]

## Slide 4: Large-scale FEM approaches in AM (2/2)
[1] Wu, W., Zhou, Y., Liu, Q., Ren, L., Fan, C., Fuh, J. Y. H., ... & Li, G. (2023). Advanced Science, 10(12), 2206486.
[2] Alvarez P, Ecenarro J, Setien I, et al. Int. J. Eng. Res. Sci, 2016, 2(10): 39-46.
(Selected as the cover of “Advanced Science 12/ 2023” Wu, W. et al)
Heating step
Cooling step
Temperature
Heat flux
Radiation
Convection
Distortion and residual stress can be accurately predicted by:
the reasonable configurations of the equivalent stress, strain, heat flux or temperature attribution.
Layer refresh

## Slide 5
Single part simulation
Kozjek, D., Porter, C., Carter III, F. M., Mogonye, J. E., & Cao, J. (2023). Journal of Manufacturing Processes.
Problems
Material deposition
Heat source
Thermal boundary
Individual specimens
Temperature field prediction
Fabrication design
Assumptions & Simplifications:
Advantages:
Easy implementation
Good efficiency
(Dominik and Conor)
Problems
(Kozjek et al.)
Multiple parts:
Geometry feature
Scan pattern
Interlayer heat variation

## Slide 6
Kozjek, D., Porter, C., Carter III, F. M., Mogonye, J. E., & Cao, J. (2023). Journal of Manufacturing Processes.
Objective of this research
Multiple specimens simulation:
Reasonable thermal boundary;
Incorporation of scan pattern;
Easy implementation;
Good accuracy.
Specimen cluster
Substrate
Whole build:
1633 layers
67 tracks
=
107 millions of tracks
(Dominik and Conor)

## Slide 7: Proposed modeling framework
Track-wise deposition
Single layer
Calculate temperature pattern T
CAD files
Heat source parameters
Start
Layer thickness
Track-by-track simulation
Heat flux attribution
Single layer(S)
Calculate temperature pattern T’
Determine heat flux Q
T’
Yes
No
Equivalent heat flux Qe (S)
Equivalent heat flux determination
Layer-wise element activation and heat flux attribution
Temperature field of whole build
End
Part geometry and building speed
Large-scale simulation

## Slide 8: Proposed modeling framework
Heat source
(Gaussian distributed)
Substrate
Cooling
Cooling
Equivalent heat flux
(Uniformly distributed)
Substrate
Temperature pattern T
Temperature pattern T’
T
Model 1: Track-by-track heating
Model 2: layer-wise heat flux attribution

## Slide 9: Governing equations
Surface heat flux
Energy balance
V: volume of solid material (m3)
S: surface area (m2)
: density of the material (kg/m3)
: material time rate of internal energy (W/kg)
q: heat flux per unit area, flow into body (W/m2)
r: heat supplied externally into the body (W/m3)
Track-by-track scanning:
Uniform distribution:
Radiation
A: radiation constant (W/(m2K4))
: sink temperature (K)
: absolute zero on temperature scale (K)
Surface convection
h: film coefficient (W/(m2K))
Constitutive definition
In terms of specific heat:
Heat conduction by Fourier law:

## Slide 10: Circular shape
t = t0
Model 2: Equivalent heat flux attribution
t = t0 + tc
Model 1: Track-by-track heating
Heat flux Qe
Cooling
t = t0
t = t0 + tc
Temperature (K)
Scan pattern
Laser ending point
tc = 10 s

## Slide 11
Scan pattern
Laser ending point
t = t0
Model 2: Equivalent heat flux attribution
t = t0 + tc
Model 1: Track-by-track heating
Heat flux Qe
Cooling
t = t0
t = t0 + tc
Temperature (K)
The two different heating method obtain the similar temperature pattern after the cooling time tc.
(under the same thermal boundary conditions)
If Qe is properly selected:
Rectangular shape
tc = 10 s

## Slide 12: Heat transfer analysis on a single layer
Preheating (K) | Qe (W/m2) | Temperature after cooling (K) | Residual temperature with Qe=29.2 W/m2
300 | 29.2 - 29.3 | 785.6 | 785.6
500 | 28.2 - 28.3 | 802.7 | 803.2
700 | 27.8 - 27.9 | 856.5 | 857.1
Qe at preheating temperature
(circular radius 3.75 mm)
Chart: Circle radius (mm)
| 2.5 | 3.75 | 5
 | 45.5 | 29.2 | 20.4
Qe at different radius
(preheating 300 K)
Residual temperature: the preheating for the next layer

## Slide 13: Heat transfer analysis on a single layer
To make the similar , Qe is primarily depending on
laser parameters
cross section area S
Assumption:
residual temperature
Heating (Qe)
Cooling (Qc)
residual temperature for next deposition
temperature after heating
Area= latent heat
Solidus
Liquidus
Temperature change:
U: energy
c: specific heat
m: mass
(Rough estimation)

## Slide 14: Part-scale heat flux attribution
Track-by-track heating
Uniform distributed heat flux
2~3 CPU hours
Within 1 min
Computational cost (per layer):
Building direction
Thermal load
Thermal boundary condition
LPBF:
Thermal conduction of the powder particles cannot be simplified as radiation and convection

## Slide 15
Group 1
Group 2
Group 3
Group 4
a
b
c
Model geometry of the specimen clusters
Powder block
Fatigue samples
Target fabrications
(By Conor Porter)

## Slide 16
Track-scale simulation:
scan speed: 1550 mm/s
laser power: 240 W
absorptivity: 0.45
material: AlSi10Mg
hatch distance: 150 um,
layer thickness (nominal): 30 um
scan path: bio-directional
cross section shape: circular
Qe(S)
[1] Wei L C, Ehrlich L E, Powell-Palm M J, et al., Additive Manufacturing, 2018, 21: 201-208. (0.2-0.3 %)
[2] Jacob G, Donmez A, Slotwinski J, et al., 2016, 27(11): 115601. (84% density)
Mesh:
Total element numbers: 868’364
Element type: DC3D10
Powder block
Specimen
Substrate
Model construction
Layer-wise element progressive activation +
Apply Qe on specimen cross sections
Part-scale simulation:
S: cross section area

## Slide 17
Temperature results
Specimen
Whole build
Specimen cluster
Single part
Layer-wise element progressive activation + Layer-wise heat flux attribution
Temperature evolution during the fabrication procedure
Cross comparison
Computational cost: 20 ~30 mins
Computational cost: 5~15 mins

## Slide 18
Temperature results
Temperature distribution after heating (example: Group 4)
Specimen cluster
Single part simulation (for comparison)
Powder block
Specimens
Same geometry & Thermal load
Different temperature distribution
Center region:
Small cooling rate
Heat accumulation
High temperature on the specimen in the center region.
Temperature field during manufacturing
a
b
c

## Slide 19
Lane B, Jacquemetton L, Piltch M, Beckett D. Thermal calibration of commercial melt pool monitoring sensors on a laser powder bed fusion system. NIST Advanced Manufacturing Series 2020;100(35):100-35.
Experiment design
(by Dominik and Conor)
Machine: DMG MORI LASERTEC 12 SLM (LT 12 SLM)
Powder: TEKMAT™ AlSi10Mg-63/20-AMS (TEKNA, Montreal, CA)
Target specimens

## Slide 20
Lane B, Jacquemetton L, Piltch M, Beckett D. Thermal calibration of commercial melt pool monitoring sensors on a laser powder bed fusion system. NIST Advanced Manufacturing Series 2020;100(35):100-35.
Experiment design
(by Dominik and Conor)
(Lane et al., 2020)
Coaxial photodiode system
Molten pool temperature measurements (TEP)
x [mm]
y [mm]
TEP [°C]

## Slide 21
Luo X, Zhao M, Li J, et al. Numerical study on thermodynamic behavior during selective laser melting of 24CrNiMo alloy steel[J]. Materials, 2019, 13(1): 45.
Preheating and melt pool temperature relation
Experimental measurement
Average molten pool temperature
(Luo X. et. al.)
Simulation temperature field
Residual temperature after heating
(Preheating of next layer)
VS
When the preheating temperature increases from 25 ℃ to 400 ℃,
the molten pool central temperature increases from 2621 ℃ to 2914 ℃.

## Slide 22
Measured molten pool temperature
Experimental measurement (by Dominik and Conor)
Chart: Layer number
Chart: Layer number

## Slide 23
Measured molten pool temperature
Experimental measurement (by Dominik and Conor)
Chart: Layer number
Chart: Layer number

## Slide 24
Comparison of simulation and experiment results
Multiple parts simulation VS Experiments
Chart: Group 1-a
Simulation | 385 | 387 | 585 | 713 | 757 | 587 | 702 | 750 | 645 | 678 | 714 | 764 | 602 | 737 | 635 | 658 | 718 | 536 | 641 | 504 | 626 | 536 | 647 | 583 | 614 | 725 | 622 | 657 | 619 | 579 | 649 | 620 | 662 | 739 | 665 | 710 | 641 | 800
Chart: Group 1-b
Simulation | 303 | 387 | 585 | 712 | 656 | 585 | 621 | 747 | 767 | 677 | 654 | 758 | 703 | 731 | 765 | 622 | 711 | 662 | 635 | 702 | 618 | 630 | 634 | 580 | 676 | 685 | 622 | 646 | 699 | 619 | 572 | 725 | 656 | 782 | 713 | 733 | 752 | 769 | 680 | 764
Chart: Group 1-c
Simulation | 306 | 387 | 585 | 512 | 556 | 585 | 622 | 749 | 568 | 678 | 612 | 561 | 602 | 633 | 651 | 723 | 683 | 790 | 580 | 630 | 503 | 617 | 534 | 539 | 634 | 481 | 607 | 611 | 519 | 664 | 600 | 717 | 638 | 601 | 658 | 729 | 658 | 680 | 658 | 854
Group 1
Local fluctuation due to:
large element size
large time step
activation of the new elements
thermal interactions

## Slide 25
Comparison of simulation and experiment results
Chart: Group 2-a
Simulation | 301 | 385 | 387 | 586 | 713 | 756 | 785 | 644 | 833 | 605 | 651 | 754 | 702 | 727 | 811 | 616 | 681 | 694 | 778 | 724 | 606 | 636 | 611 | 548 | 560 | 607 | 637 | 564 | 575 | 784 | 763 | 793 | 917 | 834 | 718 | 830 | 556
Chart: Group 2-b
Simulation | 421 | 387 | 586 | 712 | 755 | 784 | 643 | 731 | 703 | 752 | 702 | 623 | 756 | 715 | 740 | 793 | 777 | 717 | 705 | 733 | 708 | 645 | 655 | 749 | 560 | 697 | 719 | 671 | 784 | 751 | 778 | 800 | 627 | 820 | 608 | 809 | 550
Chart: Group 2-c
Simulation | 321 | 385 | 387 | 586 | 712 | 755 | 783 | 616 | 761 | 574 | 649 | 736 | 761 | 593 | 727 | 760 | 615 | 642 | 694 | 576 | 719 | 706 | 611 | 597 | 609 | 657 | 657 | 752 | 598 | 701 | 718 | 574 | 790 | 707 | 766 | 789 | 810 | 633 | 712 | 716
Chart: Group 3-a
Simulation | 321 | 385 | 387 | 661 | 655 | 683 | 615 | 676 | 630 | 577 | 706 | 658 | 662 | 595 | 645 | 611 | 511 | 668 | 517 | 508 | 638 | 537 | 537 | 547 | 660 | 608 | 630 | 691 | 618 | 562 | 672 | 573 | 728 | 673 | 629 | 720 | 612 | 709
Chart: Group 3-b
Simulation | 302 | 587 | 585 | 711 | 659 | 615 | 675 | 728 | 676 | 704 | 736 | 657 | 593 | 643 | 607 | 610 | 666 | 586 | 673 | 707 | 607 | 610 | 634 | 635 | 670 | 720 | 678 | 596 | 742 | 553 | 686 | 618 | 644 | 749 | 669 | 617 | 748 | 619 | 813 | 604 | 793
Chart: Group 3-c
Simulation | 361 | 386 | 585 | 754 | 781 | 643 | 675 | 828 | 777 | 704 | 738 | 760 | 695 | 644 | 810 | 611 | 667 | 648 | 716 | 608 | 608 | 635 | 636 | 669 | 721 | 580 | 597 | 745 | 601 | 624 | 718 | 647 | 768 | 771 | 726 | 755 | 862 | 725 | 713 | 765 | 709 | 804 | 749

## Slide 26
Comparison of simulation and experiment results
Chart: Group 2-a
Simulation | 301 | 385 | 387 | 586 | 713 | 756 | 785 | 644 | 833 | 605 | 651 | 754 | 702 | 727 | 811 | 616 | 681 | 694 | 778 | 724 | 606 | 636 | 611 | 548 | 560 | 607 | 637 | 564 | 575 | 784 | 763 | 793 | 917 | 834 | 718 | 830 | 556
Chart: Group 2-b
Simulation | 421 | 387 | 586 | 712 | 755 | 784 | 643 | 731 | 703 | 752 | 702 | 623 | 756 | 715 | 740 | 793 | 777 | 717 | 705 | 733 | 708 | 645 | 655 | 749 | 560 | 697 | 719 | 671 | 784 | 751 | 778 | 800 | 627 | 820 | 608 | 809 | 550
Chart: Group 2-c
Simulation | 321 | 385 | 387 | 586 | 712 | 755 | 783 | 616 | 761 | 574 | 649 | 736 | 761 | 593 | 727 | 760 | 615 | 642 | 694 | 576 | 719 | 706 | 611 | 597 | 609 | 657 | 657 | 752 | 598 | 701 | 718 | 574 | 790 | 707 | 766 | 789 | 810 | 633 | 712 | 716
Chart: Group 3-a
Simulation | 321 | 385 | 387 | 661 | 655 | 683 | 615 | 676 | 630 | 577 | 706 | 658 | 662 | 595 | 645 | 611 | 511 | 668 | 517 | 508 | 638 | 537 | 537 | 547 | 660 | 608 | 630 | 691 | 618 | 562 | 672 | 573 | 728 | 673 | 629 | 720 | 612 | 709
Chart: Group 3-b
Simulation | 302 | 587 | 585 | 711 | 659 | 615 | 675 | 728 | 676 | 704 | 736 | 657 | 593 | 643 | 607 | 610 | 666 | 586 | 673 | 707 | 607 | 610 | 634 | 635 | 670 | 720 | 678 | 596 | 742 | 553 | 686 | 618 | 644 | 749 | 669 | 617 | 748 | 619 | 813 | 604 | 793
Chart: Group 3-c
Simulation | 361 | 386 | 585 | 754 | 781 | 643 | 675 | 828 | 777 | 704 | 738 | 760 | 695 | 644 | 810 | 611 | 667 | 648 | 716 | 608 | 608 | 635 | 636 | 669 | 721 | 580 | 597 | 745 | 601 | 624 | 718 | 647 | 768 | 771 | 726 | 755 | 862 | 725 | 713 | 765 | 709 | 804 | 749

## Slide 27
Comparison of simulation and experiment results
Chart: Group 4-b
Simulation | 300 | 385 | 386 | 584 | 709 | 656 | 758 | 721 | 747 | 902 | 660 | 707 | 741 | 866 | 725 | 931 | 698 | 834 | 669 | 732 | 698 | 741 | 830 | 714 | 674 | 590 | 776 | 625 | 749 | 612 | 733 | 828 | 745 | 682 | 790 | 725 | 735 | 833 | 815 | 896 | 804 | 795 | 655
Chart: Group 4-c
Simulation | 314 | 385 | 386 | 584 | 709 | 758 | 618 | 748 | 757 | 814 | 707 | 741 | 869 | 700 | 722 | 750 | 715 | 731 | 685 | 769 | 713 | 800 | 639 | 555 | 715 | 675 | 589 | 677 | 714 | 750 | 676 | 725 | 764 | 771 | 686 | 715 | 743 | 843 | 712 | 696 | 769 | 684 | 556
Chart: Group 4-a
Simulation | 342 | 385.291 | 686.814 | 484.823 | 660 | 621 | 766 | 623 | 717 | 748 | 759 | 614 | 708 | 873 | 701 | 702 | 633 | 685 | 669 | 715.329 | 701.7 | 639 | 733.2 | 520.354 | 676 | 495.154 | 682.7 | 714 | 652.238 | 632.155 | 541 | 767 | 759 | 691 | 631 | 855 | 713 | 698 | 688 | 810 | 558
Overall, multiple parts simulation and experimental measurement show a similar trend.
The results indicates:
the potential relationship between preheating and molten pool temperature;
the thermal interaction effects by the heat conduction of inter-specimen powders;

## Slide 28
Chart: Specimen height (mm)
Comparison of simulation and experiment results
Heat transfer simulation
Experiment specimen
Group 4-a
Group 4-b
Group 4-c
Simulation (normalized):
Experiment (normalized):
Single part simulation VS Experiments (by Dominik)
z
For the single part simulation:
no thermal interaction
unreasonable thermal boundary conditions
Chart: Specimen height (mm)
Chart: Specimen height (mm)

## Slide 29
Chart: Group 4-b
Simulation | 300 | 385 | 386 | 584 | 709 | 656 | 758 | 721 | 747 | 902 | 660 | 707 | 741 | 866 | 725 | 931 | 698 | 834 | 669 | 732 | 698 | 741 | 830 | 714 | 674 | 590 | 776 | 625 | 749 | 612 | 733 | 828 | 745 | 682 | 790 | 725 | 735 | 833 | 815 | 896 | 804 | 795 | 655
Chart: Group 4-c
Simulation | 314 | 385 | 386 | 584 | 709 | 758 | 618 | 748 | 757 | 814 | 707 | 741 | 869 | 700 | 722 | 750 | 715 | 731 | 685 | 769 | 713 | 800 | 639 | 555 | 715 | 675 | 589 | 677 | 714 | 750 | 676 | 725 | 764 | 771 | 686 | 715 | 743 | 843 | 712 | 696 | 769 | 684 | 556
Chart: Group 4-a
Simulation | 342 | 385.291 | 686.814 | 484.823 | 660 | 621 | 766 | 623 | 717 | 748 | 759 | 614 | 708 | 873 | 701 | 702 | 633 | 685 | 669 | 715.329 | 701.7 | 639 | 733.2 | 520.354 | 676 | 495.154 | 682.7 | 714 | 652.238 | 632.155 | 541 | 767 | 759 | 691 | 631 | 855 | 713 | 698 | 688 | 810 | 558
Multiple .vs. single part (Group 4)
Chart: Specimen height (mm)
Chart: Specimen height (mm)
Chart: Specimen height (mm)
Multiple parts
Single parts

## Slide 30
Comparison of simulation and experiment results
 | a | b | c
Group 1 | 0.48 | 0.66 | 0.6
Group 2 | 0.32 | 0.43 | 0.14
Group 3 | 0.35 | -0.76 | -0.09
Group 4 | 0.34 | 0.53 | 0.44
 | a | b | c
Group 4 | -1.2 | -2.59 | -3.31
R2 (Single part simulation VS Experiments)
R2 (Multiple parts simulation VS Experiments)
(by Dominik)
R2 (coefficient of determination)
RSS= sum of squared residuals
TSS= total sum of squares
Normalization
: large difference

## Slide 31
Feasibility in large-scale thermal modeling
Multiple islands heating test:
Model geometry
Two different heating configurations

## Slide 32
Feasibility in large-scale thermal modeling
Model 1: Track-by-track heating
Heating procedure
4th island
1st island
Heating end point
Heating end point
Heating procedure
Short period of cooling
Short period of cooling
Thermal loading direction
Model 2: Equivalent heat flux attribution
Similar residual temperature pattern
Similar residual temperature pattern
High thermal conductivity,
Rapid scan speed,
Large island area,
Heating by equivalent heat flux attribution always produces a temperature pattern similar to that achieved by track-by-track heating.

## Slide 33
7th island
12th island
Heating end point
Heating end point
Feasibility in large-scale thermal modeling
Model 1: Track-by-track heating
Heating procedure
Heating procedure
Short period of cooling
Short period of cooling
Model 2: Equivalent heat flux attribution
Similar residual temperature pattern
Similar residual temperature pattern
High thermal conductivity,
Rapid scan speed,
Large island area,
Heating by equivalent heat flux attribution always produces a temperature pattern similar to that achieved by track-by-track heating.

## Slide 34
Feasibility in large-scale thermal modeling
Strategy 1
Temperature difference
Strategy 2
Observations:
1. Scan orientation affects residual temperature pattern;
2. Prediction error can be accumulated with cross-section area
3. Prediction error is tolerable compared to the global temperature change.

## Slide 35
Highlights & Summary
Development of an integrated part-scale modeling framework that combines layer-wise equivalent heat flux attribution with layer-wise element activation.
Justification of the equivalent heat flux through high-fidelity track-scale simulations.
Incorporation of the inter-specimen heat conduction effects through the powder bed.
Remarkable consistency of the simulated temperature data obtained from each equivalent layer compared to the experimental observations
A rational explanation for the different temperature distributions and cooling rates observed in samples with identical geometries but at different position.
A sound physical basis and excellent computational efficiency.

## Slide 36
Future work
Thermal interaction:
Incorporating depositing sequence for cross sections of different samples;
Data-driven approaches:
Predicting Qe and temperature curves using machine learning approaches;
Different part shape:
Analyzing the effects of various cross-section shape.

## Slide 37
Acknowledgements
Department of Defense Vannevar Bush Faculty Fellowship
Notes: Thank you for your attention!
Any questions, comments, or suggestions are welcome.