## Slide 1: Data-driven prognostic model for temperature field in additive manufacturing based on the high-fidelity thermal-fluid flow simulation
Supervisor: Prof. Wentao YAN
Email: mpeyanw@nus.edu.sg
Fan CHEN
(4th year PHD student)
Email: e0348805@u.nus.edu

## Slide 2
Problem
Thermal-fluid flow simulation
Grain growth
Thermal stress
High computational cost of the thermal-fluid flow simulation;
Complex pre-processing of the temperature profiles;
High computational cost of the temperature loading.
Data-driven model
P, v
T
Fluid dynamics
Heat transfer
Powder bed fusion (PBF)
Phase transfer:
Melting and solidification
Evaporation, etc.
Heat transfer:
Heat absorption
Heat conduction, radiation, etc.
Fluid dynamics:
Marangoni convection
Capillarity, etc.

## Slide 3
Overall framework
INPUT:
manufacturing parameters
OUTPUT: isotherm dimensions to reconstruct temperature field
Regression/machine learning algorithms
Training data: thermal-fluid flow simulation
Discretize & extract
Isotherms
y
x
z
Isothermal points of ± ∆T
y
x
z
Curve fitting &
parameterization
Curve 1:
Curve 2:
O
Curve-fitting of the isothermal points at the layer
Region 1
Region 2
Data preparation
EVALUATION:
Thermal stress model/
Grain growth model

## Slide 4
Training data: thermal-fluid flow simulation
y
x
z
Isothermal points of ( ± ∆T ) K
y
x
z
Discretize & extract
y
x
z
Isotherms
Curve fitting & parameterization
O
Curve-fitting of the isothermal points at the layer
Model construction
Output variables:
Temperature field parameterization

## Slide 5
1560 K
1000 K
temperature contours
=
=
y
x
Below 1000 K, the solid-state phase transformations barely occur and the residual stresses do not change much.
One of the layers
y
x
z
Accuracy of the isotherms extraction
Half-width b captured inaccurately: Different contours share the same half-width b due to the limited mesh size.
b
Two main factors:
Contour numbers
Mesh size of the simulation
The grain evolution and thermal stress are essentially determined by the temperature field at and around the molten pool boundary (1000~1560 K).
(Inconel 625)
Model construction

## Slide 6
Symmetric central line
Maximum-width position
Maximum-width segment
y
x
Fitting of the isothermal points of ( ± ∆T) K
Model construction
Temperature field parameterization
Output variable:
Curve shape and temperature gradient in two regions are quite different.
Split line
Region 1
Region 2
± ∆T1
± ∆T2
Reference point

## Slide 7
Model construction
Well aligned
Irregular
The two endpoints E1, E2 are highly irregular;
The center points (E1+E2)/2 are well aligned.
Reference lines
x
z
Base point
Free surface
Longitudinal symmetric plane
Output variables:
Fitting reference line
L layers
Fixed layer distance
Combination of the isotherms
3D view
y
x
z
Fitting of the reference lines
x
z

## Slide 8
Chart: 
| 1 | 2 | 4 | 1 | 2 | 4 | 0.5 | 1.5 | 2 | 0.5 | 1 | 2 | 0.2 | 1.0469999999999999 | 0.68799999999999994 | 1.6850000000000001 | 0.2 | 0.5 | 0.5 | 0.5 | 0.8 | 0.5 | 0.5 | 0.8 | 1.2 | 0.5 | 1.2 | 0.6 | 1.8 | 0.7 | 1.5 | 0.8 | 1.2 | 1.8 | 1.2 | 1.8 | 1.5 | 1 | 0.8 | 1.6 | 1 | 1
 | 100 | 100 | 100 | 120 | 120 | 120 | 40 | 80 | 40 | 80 | 80 | 80 | 17.3 | 51 | 63 | 89 | 40.4 | 42.1 | 47.6 | 42.5 | 42.6 | 63 | 85 | 65.4 | 66.9 | 70.8 | 45 | 50 | 50 | 55 | 55 | 60 | 60 | 60 | 65 | 65 | 70 | 70 | 75 | 75 | 40 | 85
Input: manufacturing parameters for the thermal-fluid flow simulation samples
Output: the geometry features of the isotherms
Model construction
Data-driven algorithms
(Samples. No.1 ~42, Each case costs about 100 CPU hours)
(Inconel 625)
Velocity (m/s)
Power (W)

## Slide 9
Model construction
Data-driven algorithms
Gaussian process regression (GPR)
Quadratic regression (QR)
Feedforward neuronal network
Support vector regression (SVR), Linear regression (LR)
Two main factors:
High accuracy
Fast predicting speed

## Slide 10
Model setting
Fitting function for isotherms
O
Ellipse function:
Polynomial function:
Curve 2
Ellipse function
Curve 1
Ellipse function
Mean square errors:
Fitting performance
(Tested on No. 1~ No. 26)
Region 1
Region 2

## Slide 11
Polynomial fitting
Ellipse fitting
Polynomial fitting
Ellipse fitting
Region 2:
Region 1:
Isothermal points in thermal-fluid flow simulation
1000 K
1050 K
1110 K
1340 K
1270 K
1560 K
Fitting performance of different functions
Model setting
10th layer of sample no. 26

## Slide 12
Performance (MSE) of different algorithms on different output variables
Model setting
Layer numbers L
Slope angle θ
L layers
Training data sets: no.1~ no.26

## Slide 13
Model setting
Relative distance ∆x
Relative distance
Range (10-9 m2)
Range (10-9 m2)
Range (10-9 m2)
O
Performance (MSE) of different algorithms on different output variables
Training data sets: no.1~ no.26

## Slide 14
Testing Sample no. 41
V =1 m/s
P =40 W
Different training datasets
Predicted isotherms of Region 2
Model setting

## Slide 15
j th layer
( j+1)th layer
G
Isotherms
Global base line lb
lhigh
llow
Horizontal planes
Temperature calculation by the interpolation
Predicted isotherms
Temperature field reconstruction
y
x
z
y
x
z
j th layer
( j+1)th layer
G
Local coordinate system in plane
Global base line lb
Model evaluation
Temperature field reconstruction
B

## Slide 16
(Gas)
Model evaluation
y
x
z
Temperature difference
Region 2 (<100K)
Over-prediction of the molten pool half-length a1
Region 1 (> 300K)
Predicted results
CFD results
Temperature history
Training: No. 1~40
Testing Sample: no. 41, V =1 m/s, P =40 W
y
x
z
(Inconel 625)
(Index1, Index2) for the isotherms: (5, 4) & (6, 3)
Deviation: 0~100 K
Under-prediction of width (b)
Over-prediction of depth (L)

## Slide 17
Model evaluation
Thermal stress history on node P
(Similar trend and level)
Deviation: 0~30 MPa

## Slide 18
Model evaluation
Thermal stress history on node P
Due to the small level of the Y-Y and Z-Z stress components, the deviations affect less on the Mises-stress.

## Slide 19
Model evaluation
Grain growth
Ground truth
Prediction
Less grains with high aspect ratios in the prediction due to the under prediction of the molten pool depth.
Average grain volume:
Data-driven prediction: 1032.2μm3
Ground truth: 1285.5μm3.
Deviation: 19.7 %
Training: No. 1~40
Testing Sample no. 42, V =1 m/s, P =85 W

## Slide 20
Computational cost
The computational cost of the data-driven predicted model is reduced by at least 70 %.
Temperature (K)
The simulation case with 1400+ steps can be finished within 36 CPU hours, which is nearly impossible for other thermo-mechanical models.
No heat transfer
No thermal-fluid flow calculation
No CFD temperature files loading
Data-driven predicted 5-track 3-layer AM case
Application:

## Slide 21: Thank you
Fan Chen
Email: e0348805@u.nus.edu
Fan Chen, Min Yang, Wentao Yan*, Data-driven prognostic model for temperature field in additive manufacturing based on the high-fidelity thermal-fluid flow simulation. (under review)
Yan group website: https://blog.nus.edu.sg/yanwt/